# Internal battery RB (6.4V/36Ah)

Pack of 36 LiFePO4 rechargeable batteries to install into Hub BP Jeweller

| ### Battery type | Batteries 36 × IFR18650 Rechargeable lithium iron phosphate (LiFePO4) battery cells. Battery configuration 2S18P Nominal voltage 6.4 V⎓ Capacity 36 Ah |
| --- | --- |
| ### Power supply | Maximum load current 3,000 mA End-of-life battery voltage 4.5 V⎓ |
| ### Charge and discharge conditions | Charge temperature range from 0 °C to +45 °C from 32 °F to 113 °F Charge relative humidity 60 ±25% Discharge temperature range from −25 °C to +65 °C from −13 °F to 149 °F Discharge relative humidity 60 ±25% |
| ### Storage conditions | Storage temperature range from −20 °C to +45 °C from −4 °F to 113 °F Storage humidity 60 ±25% |
| ### Transportation and shipment | Shipment voltage 6.0–6.4 V⎓ Transportation requirements For air transportation, lithium batteries must be charged to no more than 30% of their rated capacity. The shipment voltage complies with this requirement. For other types of transportation, the battery must be transported in accordance with applicable regulations and carrier requirements. |
| ### Cautions | Do not expose the battery to open flames, sparks, or any other ignition source. Do not short the power terminals. Do not disassemble or deform the battery. Avoid excessive mechanical impact or vibration. Use the battery with compatible devices only. Hub BP Jeweller does not charge this battery. The battery must be installed fully charged. |
| ### Enclosure | Dimensions 133 × 120 × 51 mm 5.24″ × 4.72″ × 2.01″ Weight 1.52 kg 3.34 lb Battery connector type Molex 2139-2 or similar Operating temperature range from −25 °C to +65 °C from −13 °F to 149 °F Operating relative humidity from 35% to 85% |
| ### Complete set | Internal battery RB (6.4V/36Ah) Cable adapter for charging the battery |
| Warranty | 24 months |